|  | BR7 BR7 SHEETING AND ACCESSORIES SHEETING The roof sheeting / side cladding shall be the BR7 profile in ISQ 300 steel 0.58mm / 0.8mm in a galvanised spelter of Z275. The BR7 profile shall be roll-formed with 8 trapezoidal ribs at 127mm centres giving a nett cover of 889mm. The rib height shall be 38mm. FINISH FOR BR7 The profile shall be supplied in a galvanised spelter or with a paint finish consisting of a full top coat Globalcoat Silicone Modified Polyester……………….(insert colour) colour finish to one / two sides. BR7 shall be obtained from Global Roofing Solutions – Tel. (011) 898-2900 ASSEMBLY The sheeting shall be laid with side-laps on the leeward side of the prevailing wind direction. An approved side-lap sealant shall be incorporated on roofing with a pitch of less than 15 degrees. All fixing holes shall be drilled and not punched. Roof sheets shall be fixed by means of No.14 Top speed Hex Head screws 65mm LG for steel purlins or 65mm LG for timber purlins and shall incorporate 26mm diameter bonded washers. Side-lap stitching shall be effected at no more than 600mm centres with 25mm LG Top speed Hex Head screws. Side Cladding shall be fixed by means of No. 14 Hex Head screws 25mm LG for steel girts or 50mm LG for timber girts and shall incorporate 19mm diameter bonded washers. Every precaution shall be taken to prevent damage to roof sheets during all stages of construction. Duck boards should be used when necessary to protect the sheeting from damage. Sheeting which has become deformed or damaged in any way, shall be replaced. FLASHINGS Stop endings must be formed at apex to form a dam and the pan turned down to form a drip. The roof sheeting shall be closed as necessary with purpose made flashings and shall incorporate serrated closers and poly closers where necessary. Flashing shall be fixed to roofing by means of No. 14 Top speed Hex head screws 25mm LG with 26mm diameter bonded washers on roof and 19mm diameter bonded washers for side cladding. The flashings shall be supplied in a galvanised spelter or with a paint consisting of a full top coat Globalcoat Silicone Modified Polyester……………….(insert colour) to one / two sides. QUALITY ASSURANCE The manufacturer shall be assessed and certified as complying with ISO 9001: 2000 Quality Management System. SAFETY The contractor shall exercise special care when handling long length sheeting, particularly in windy conditions. Should work be interrupted for any reason, all loose sheeting and incomplete sections must be adequately secured against possible movement by wind and gravity. HANDLING AND STORAGE The contractor shall ensure that all materials used on site for cladding, etc. are transported, handled and stored in accordance with the manufacturer’s recommendations. Material damaged shall be rejected and replaced with undamaged material at the contractor’s expense. Repair of damaged material will not generally be permitted. Rates are to include for preventing damage and protecting sheets through all stages of construction. INSPECTION PRIOR TO INSTALLATION OR ERECTION Before commencing installation, the contractor shall verify that the following items have been checked and accepted: The entire structure or the portion thereof to be sheeted has been correctly aligned, levelled and grouted. Purlins and sheeting rails are at the correct spacing and are within the specified tolerances. The corners of the roof are square and the wall framework is perpendicular or as specified. No protrusions such as bolt heads, splice plates, cleats, etc. appear on the face of the framework. All members to which roofing and cladding are to be fixed in aesthetically sensitive areas are true and square. Paint and any other materials that may be incompatible with the sheeting, have been painted over or so dealt with that direct contact with the sheeting is avoided. The contact faces between the purlins or the girts and the cladding are in the same plane. Should the alignment be inadequate, the contractor shall request instructions from the engineer before proceeding with the fixing of the cladding. PROTRUSION THROUGH SHEETED SURFACES Protrusions such as pipes, ducts and the like, shall be adequately flashed where they pass through the sheeting surface. Where ribs have to be cut away to permit penetration, additional framing is to be installed as required to support the sheeting. Depending on the position of the penetration through the roof, special attention shall be given to back flashing the sheeting to the ridge or point of water entry. In all cases, all cutting and flashings shall be so arranged that adequate provision is made for the drainage of all troughs and corrugation. CLEANING OF ROOF, ETC. All debris, swarf, etc. arising from the fixing of the cladding shall be removed from the sheeting as the fixing progresses. In addition, off-cuts of insulation, surplus fasteners and sealants, mandrels from pop rivets, off-cuts of flashings and sheeting, surplus flashing, food packaging, cartons, bottles, cans, etc. shall not be left on the roof or in the gutters. Care shall be taken to ensure that no such material enters, blocks or partially impedes the flow of water into the outlets, down pipes, etc. Item Description Unit Quantity Rate Total 1. Roofing sheeting / side cladding shall be BR7 profile: ISQ 300 0.58mm in a galvanised spelter of Z275 or ISQ 300 0.8mm in a galvanised spelter of Z275 or ISQ 300 0,58mm in a galvanised spelter of Z275 and with a Globalcoat colour finish to one side or ISQ 300 0.58mm in a galvanised spelter of Z275 and with a Globalcoat colour finish to two sides or ISQ 300 0,8mm in a galvanised spelter of Z275 and with a Globalcoat colour finish to one side or ISQ 300 0.8mm in a galvanised spelter of Z275 and with a Globalcoat colour finish to two sides or Aluminium 0,8mm Mill Finish or Aluminium 0,9mm Mill Finish or Aluminium 0,8mm colour coated one side or Aluminium 0,8mm colour coated two sides or Aluminium 0,9mm colour coated one side or Aluminium 0,9mm colour coated two sides or The BR7 profile shall be installed in strict accordance with manufacturer’s specifications. Manufacturer: Global Roofing Solutions – Brownbuilt (011) 898-2900, HH Robertson (011) 392 9800. Globalcoat Standard Colours: Please contact manufacturer. Please note: Colours for Aluminium sheeting as supplied by Hulett Aluminium. M2 2. Bullnosing to a radius of…….mm (450mm min.) OR Curving to a radius of………..mm (from 800mm to 36m) Lm M2 3. Over and above for rake cutting and waste. Lm 4. Bend up troughs to form a dam. Lm 5. Bend down troughs to form a drip. Lm 6. Translucent Roofing / Side Cladding shall be Modek GRP (Fibre Glass) Heavy / Standard weight with UV surface protection in Clear/Tinted in BR7 profile fixed in strict accordance with specification. OR Translucent Roofing / Side Cladding shall be Modek Polycarbonate 1,5mm with UV protection in Clear / Tinted in Supa-Clad profile fixed in strict accordance with specification. M2 7. Roof Insulation shall be "Thermapan" Backing Panel 25mm / 40mm thick with an infill of Structabord / Isoboard. OR Foil Faced Insulation…….mm thick / Structabord …….mm thick / Isoboard …….mm thick / Alucusion / Sisalation 420SA. FLASHINGS shall be manufactured from *(Insert one of options below in this space) and fixed in strict accordance with manufacturer’s specification. *Options of finish to be placed above: 0,58mm galvanised Z275 spelter 0,8mm galvanised Z275 spelter 0,58mm galvanised Z450 spelter 0,8mm galvanised Z450 spelter 0,58mm galvanised Z275 spelter with a Globalcoat finish to one side 0,58mm galvanised Z275 spelter with a Globalcoat finish to two sides. 0,8mm galvanised Z275 spelter with a Globalcoat finish to one side. 0,8mm galvanised Z275 spelter with a Globalcoat finish to two sides. Aluminium 0,7mm Mill Finish Aluminium 0,8mm Mill Finish Aluminium 0,9mm Mill Finish Aluminium 0,7mm colour one side. Aluminium 0,7mm colour two sides Aluminium 0,8mm colour one side. Aluminium 0,8mm colour two sides. Aluminium 0,9mm colour one side. Aluminium 0,9mm colour two sides. M2 8. Ridge Cap 462mm girth 1 times bent including B/F Serrated Closers and Poly-Closers. Lm 9. Hip Cap 462mm girth 13 times bent including Serrated Closers and Poly-Closers. Lm 10. Apex Flash 462mm girth 1 times bent including Serrated Closers and Poly-Closers. Lm 11. Headwall Flash 308mm girth 1 times bent including Serrated Closers and Poly-Closers. Lm 12. Sidewall Flash 308mm girth 1 times bent. Lm 13. Curved Sidewall Flash 308mm girth 1 times bent to a radius of …………..mm. No 14. Counter Flash 154mm girth 2 times bent. Lm 15. Curved Counter Flash 154mm girth 2 times bent to a radius of …………mm. No 16. Apron Flash 308mm girth 1 times bent including Serrated Closers and Poly-Closers. Lm 17. Gable Trim (Barge Flash) 385mm girth 1 times bent. Lm 18. Curved Gable Trim 385mm girth 1 times bent to a radius of ………..mm. No 19. External Corner Trim 462mm girth 1 times bent. Lm 20. Internal Corner Trim 462mm girth 1 times bent. Lm 21. Cap Flash…………mm girth 2 times bent. Lm 22. Drip Flash 154mm girth 3 times bent. Lm 23. Back Flash (Soaker Flash)……….mm girth 2 times bent. Lm 24. Valley Gutter……….mm girth 4 times bent. Lm 25. Hood Flash…….mm girth 3 times bent. Lm 26. Door Jamb Flash 154mm girth 3 times bent. Lm 27. Window Jamb Flash 154mm girth 3 times bent. Lm 28. Window Sill Flash 154mm girth 3 times bent. Lm 29. Pipe Flash (Dektite 40mm/50mm/100mm/150mm) No Note! For special flashing requirements contact Global Roofing Solutions - Brownbuilt (011) 898-2900, HH Robertson (011) 392 9800 |  |
| --- | --- | --- |